k

- 45-C10 Hoa Hong 2 Str., Ward 2, Phu Nhuan Dist., - HCMC, Vietnam Tel: 84-8-5170273 / 875 Fax: 84-8-5170174 / 2831 Email : info@lukivietnam.com Website : www.lukivietnam.com

PRODUCT DISCRIPTION STRETCH FILM (LukiFilm # 08903)

- Product No. 	:	Stretch Film (LukiFilm # 08903)

## APPLICATIONS

- Pallet Wrapping

## TECHNICAL PERFORMANCE

| PROPERTIES |  | UNITS | VALUE | METHOD |
| --- | --- | --- | --- | --- |
| Width | / | mm | 500 | Measurement tape |
| Average thickness | / | mm | 0.019 & 0.020 (±0.001) | Thickness gauge |
| Ultimate stretch percent |  | % | > 230 | - |
| Ultimate stretch Force |  | Kgf | > 26 | - |
| Puncture Resistance |  | Kg (At 250% Prestretch) | > 1.5 | - |
| Retention Resistance | Max | Kg (At 250% Prestretch) | > 1.5 | - |
|  | End |  | > 1.0 |  |
| Tensile Strength | MD | Mpa | > 26 | ASTM D 882 |
|  | TD |  | > 17 |  |
| Elongation at break | MD | % | > 345 | ASTM D 882 |
|  | TD |  | > 555 |  |
| Quality Test | Stretch at 250% continuous run 50 meter |  | Pass | - |

## STORAGE DETAILS

- Clean and dry in well ventilated area, preferably at temperature between 100C and 300C. Stored under these conditions shelf life will be a minimum of 12 months.

IMPORTANT NOTICE

Luki makes no warranties, express or implied, including, but not limited to, any implied warranty or merchantability or fitness of a Luki product for a particular purpose. Luki is not responsible in determining the particular purpose or suitability of application on the user's behalf as the performance of the Luki product may vary under different applications and circumstances thereafter. The materials to be laminated with the product, the surface preparation procedures, choice of product, period of time and environment conditions when applied are factors which can affect the performance of the  Luki product.

Given the countless number of possibilities which may affect the performance of the Luki’s product, and some of which are within the user's knowledge and control, it is therefore essential for the user to determine whether the Luki’s product is fit or suitable for that particular purpose or method of application.

LIMITATION OF REMEDIES AND LIABILITIES

If the  Luki’s product is proven to be defective, THE EXCLUSIVE REMEDY, AT LUKI'S OPTION SHALL BE TO REFUND OR REPLACE THE DEFECTIVE Luki PRODUCT, and within the limits of the purchase price. Luki shall not otherwise be liable for any loss or damages, whether direct, indirect, special, incidental or consequential, regardless of the legal theory asserted, including negligence, warranty, or strict liability.