- 203/9 Dang Thuy Tram Str., Ward 13, Binh Thanh Dist., - HCMC, Vietnam Tel: 84-8-35534001/2/3/4 Fax: 84-8-35534005/6 Email : info@lukivietnam.com Website : www.lukivietnam.com

PRODUCT DISCRIPTION ALUMINIUM FOIL TAPE (LukiTape # 06610)

- A 41 micron (1.6mil) high tensile strength aluminum foil backing, combined with a high performance synthetic rubber-resin adhesive, protected by an easy –release silicone release paper.

## APPLICATIONS

- HVAC industry for joining and sealing Foil-Scrim- Kraft facing laminated fiberglass blanket/ duct board joints and seams; joining and sealing flexible air duct seams and connections. May also be use for other industrial uses requiring a tape with these characteristics and benefits.

## FEATURES/BENEFITS

- Aluminum backing provides excellent reflection of both heat and light,

- High quality adhesive with super strong adhesion and holding power offers reliable and durable Foil-Scrim-Kraft Facing joints and seams in HVAC ductwork application.

- Low moisture vapor transmission rate makes LukiTape#06610 an excellent vapor barrier.

- Service temperature range from -20C to 80C (-4~ +176 F)

## TECHNICAL PERFORMANCE

| PROPERTIES | METRIC | ##### ENGLISH | TEST METHOD |
| --- | --- | --- | --- |
| Backing Thickness | 16 Micron | 0.64 Mil | PSTC-133 / ASTM D 3652 |
| Total Thickness | 41 Micron | 1.6 Mil | PSTC-133 / ASTM D 3652 |
| Adhesion to Steel | 25N/25mm | 90 Oz./In. | PSTC-101 / ASTM D 3330 |
| Tack Rolling Ball | 20 cm | 8.0 In. | PSTC-6 / ASTM D 3121 |
| Tensile Strength | 75 N/25mm | 17.0 Lb/In | PSTC-131 / ASTM D 3759 |
| Elongation | %. | 3.5 | PSTC-131 / ASTM D 3759 |
| Service Temperature | -20  +80 C | -4 ~ +176 F | ------------ |
| Applying Temperature | +10 ~ 40 C | +50 ~ +105 F | ------------ |

## Tolerance:

## Weight and thickness: ± 10%;

## STORAGE AND SHELF LIFE DETAILS

- 12 months when stored at 21C (70F) / 50% relative humidity out of direct sunlight.

SURFACE PREPARATION:

- It is essential, as with all pressure-sensitive tapes, that the surface to which the tape is applied must be clean, dry, free of grease, oil or other contaminants.

PRODUCT USE:

- It is essential that the user evaluate the LukiTape product to determine whether it is fit for a particular purpose and user’s method of application. Good results will be obtained when applied to a clean, dry surface with a suitable pressure on LukiTape product between +10 ~ +40°C (+50 ~ +105 F).

AUTHORIZED REPRESENTATIVE

IMPORTANT NOTICE

Luki makes no warranties, express or implied, including, but not limited to, any implied warranty or merchantability or fitness of a Luki product for a particular purpose. Luki is not responsible in determining the particular purpose or suitability of application on the user's behalf as the performance of the Luki product may vary under different applications and circumstances thereafter. The materials to be laminated with the product, the surface preparation procedures, choice of product, period of time and environment conditions when applied are factors which can affect the performance of the  Luki product.

Given the countless number of possibilities which may affect the performance of the Luki’s product, and some of which are within the user's knowledge and control, it is therefore essential for the user to determine whether the Luki’s product is fit or suitable for that particular purpose or method of application.

LIMITATION OF REMEDIES AND LIABILITIES

If the  Luki’s product is proven to be defective, THE EXCLUSIVE REMEDY, AT LUKI'S OPTION SHALL BE TO REFUND OR REPLACE THE DEFECTIVE Luki PRODUCT, and within the limits of the purchase price. Luki shall not otherwise be liable for any loss or damages, whether direct, indirect, special, incidental or consequential, regardless of the legal theory asserted, including negligence, warranty, or strict liability.